## Slide 1: Big, Deep, and Smart Data in Imaging – Towards Nanoscience 2.0
Guiding the design of materials tailored for functionality
Sergei V. Kalinin
Institute for Functional Imaging
of Materials

## Slide 2: Opportunities in Materials Science
Renewable energy, self-driving cars, transparent displays, new memory technologies
Need for new materials not being met by classical approach
Notes: Make first slide opening – put some pictures of solar cells, cars, etc (Julia Greer style). Space elvator if you want. Amd then put Ceder Nature Mat paper (just cut and paste from pdf)
So this slide is opportunity. Next is limitaitons
When you talk, make message very clear.
------
Good afternoon everyone. Materials have driven new technology, and continue to do so at a frantic pace today. They are required to meet the energy challenges of our time, to solve social problems such as traffic and road fatalities, and for consumer goods including better, faster memory devices and transparent and flexible screens for electronics. However, the traditional paradigm for discovering new materials is outdated. Traditionally, people would synthesize new materials based on a combination of serendipity, intuition, and knowledge of the related compounds. However, with increasing complexity of the materials that are beign synthesized, the possible combinations also increase exponentially and this approach is no longer viable. Therefore, we need a new method, which was first introduced about a decade ago – that is, predicting properties by merging data science with first principles calculations.

## Slide 3: More than imaging
Atomic positions can be determined to <10-pm precision
Bond length: Chemical reactivity, catalytic activity
Bond angles: Magnetism and transport
Configurations and repeating elements?
J.J. Guo et al., Nat. Comm. 5, 5389 (2014)
Nature 515, 487 (2014)
Notes: The concept we propose is a “genome” that has one strand being atomic and mesoscopic imaging, and another theory, with big data playing a role of the binding groups. Connections are unsupervised learning, correlative learning, image recognition, supervised learning

## Slide 4
Dynamic matter: information dimension
Static matter
Functional matter
Dynamic matter
Controlled matter
Unsupervised
learning
Theory
Correlative
learning
Image
recognition
In-situ Control
Big data
Imaging
Electronic Structure
Molecular Dynamics
Multiscale
Ab Initio dynamics
Notes: The concept we propose is a “genome” that has one strand being atomic and mesoscopic imaging, and another theory, with big data playing a role of the binding groups. Connections are unsupervised learning, correlative learning, image recognition, supervised learning

## Slide 5: Imaging: What do the atoms do?
  Classical concept
  Synthesis
  Characterization
  Theory
  Computation
  Expanding to include
  Data mining
  Correlative functional imaging
  Local theory-experiment matching of multi-dimensional (multi-modal), spatially and temporally resolved information
  Institute for Functional Imaging of Materials (IFIM)
  Develop new imaging probes and workflows based on synergy
  between imaging disciplines
  Bridge physical imaging with theory via big data and data analytics to design new materials
  Leverage ORNL strengths in
    Physics and chemistry on the atomic scale in real space
    Mesoscale structure and functional probing
    Big data and predictive theories
Our scientific paradigm is shifting
Notes: What is new now compared to the past? Why is it opportunity
Imaging becomes a source of quantitative measurements, rather then just pictures
Caveat: we have a lot of data, but relatively high noise.
Need to find ways to get use it, complement with functional probing, and link to local and global properties

## Slide 6: Approach
Unsupervised learning, clustering, and visualization
Biggest hurdle: Language/ elementary tools
1. Big data: How does it happen?
Physics informed data analytics/ supervised methods
Biggest hurdles: Mathematical framework, scalability of computational tools
2. Deep data: How can we understand?
Feedback and expert/AI systems
Biggest hurdles: Don’t know where to start, but it is possible
3. Smart data: How can we do better?
Physics: Why something happens

## Slide 7
Level 1: Big data in imaging

## Slide 8
Imaging:
A. Borisevich
Q. He
Sample:
V. Guilants
Image analysis:
S. Jesse
A. Belianinov
Notes: Figure 2. Two phase Mo-V-M-O (M = Nb, Ta, Te and/or Sb). (a) M1 and M2 mixed phase STEM image. (b) k-means clustering results for 6 neighbor, sort by distance metric case. (c) k-means clustering results for 6 neighbor, sort by angle metric case. (d) FFT of image in (a). (e) 50 member neighborhood of the image in (a). (f) 6 member neighborhood of the image in (a). (g) Dendrogram for the 6 neighbor, sort by distance metric case.

## Slide 9
Normal Modes Analysis
PCA transforms the data such that the greatest variance by any projection lies on the first coordinate
k-means clustering aims to partition the n observations into k sets (k ≤ n) S = {S1, S2, …, Sk} so as to minimize the within-cluster sum of squares
Principal Component Analysis
K-means Clustering
Chemistry
Physics

## Slide 10
Local Chemistry: K-means
All Clusters
Cluster I
Cluster II
Cluster III

## Slide 11
11
13
3
-3
2
-2
2
-2
Local Physics: PCA
Raw Data
Clustering
PC I
PC II
PC III
PC IV

## Slide 12
Image Analytics: Enabling the Discovery
Image based analysis for quantitative improvement of Molybdenum–Vanadium based complex oxide catalysts for propane ammoxidation
Identification of new phases undetectable by visual inspection
Link to catalytic properties?
Q He, J Woo, A Belianinov, VV Guliants, A Borisevich; ACS nano, DOI: 10.1021/acsnano.5b00271, (2015)

## Slide 13
15°
a
b
a
1.5
2.3
0
3 nm
3 nm
STM image of FeSeTe at L-He
Superconductive gap map
Filtered STM Image
Local unit cell volume
The defect preserves lattice continuity, but is associated with change in molar volume and lattice parameter - Guinier-Preston zone. Superconductivity is suppressed at the defect.
Local property mapping
Notes: 13

## Slide 14: Materials Carthography
Curtarolo:
Electronic structure fingerprints
Structural elements favorable for superconductivity
Key to rational materials design

## Slide 15: Local structure-property coupling
Surface atomic structure
Tunneling spectral image
Structure descriptors:
Atom height
Molar volume
….
Electronic property descriptors:
PCA components of spectra
Superconductive gap
….
T. Gianfrancesco, CIRE student (supported by this proposal)

## Slide 16
Phase 1
Phase
2
Image
Positions
Physics
Structure
3D
4D
5D
Spectra
Multivariate
Analysis
Properties
Physics and chemistry on single defect level
Identify &
Classify
Structure
Analysis
Register & Deconvolute
Genomic
Library
Atomic-Scale Structure and Functionality
Need new language:
What are structural descriptors?
How do we define local symmetry, phases and ferroic variants?
How do we introduce and quantify translational symmetry?
What do we learn:
Structure-property relationship on single atom, molecule, and defect level
Libraries of structure-property relationships
Feedback to theory through microscopic degrees of freedom
Scattering methods: completeness of library
Macroscopic properties: averaging rules

## Slide 17
Materials Genome
Big data in theory: new opportunities for science (Materials Genome)
Problems:
Both number of combinations and computational complexity diverge exponentially with system size
No feedback from experiment/theory refinement
Practical realization
Many functionalities are defined on length scale well above unit cell
Perovskite
Spinel
Notes: http://ascr-discovery.science.doe.gov/feature/jain2.shtml
http://commons.wikimedia.org/wiki/File:Perovskite_ABO3.jpg
http://www.tf.uni-kiel.de/matwis/amat/def_en/kap_2/basics/b2_1_6.html

## Slide 18: Imaging to genome
“Stochastic” library
Future:
Libraries of preferred local configurations: what is relevant
Structural + functional imaging: stochastic combinatorial libraries
Refining the theory
Classical approach: Synthesis → Characterization → Theory
Need:
Functional probes
High-resolution structural imaging
Theoretical models
Big/Deep/smart data
Tm
γ
Y
P
Ρ
…
Bulk Crystal
Chemical Space
Functional Properties
φ (x,y,V,…)
Y (x,y,V,…)
P (x,y,V,…)
…
Big data from imaging:
Notes: http://ascr-discovery.science.doe.gov/feature/images/jain_fig1.gif

## Slide 19
Level 2: Deep Data
“Theoretical microscope”
Physics-constrained unmixing
Inverse problems

## Slide 20
Mesoscale
Atomistic Imaging
Mesoscale Imaging
Atomistic Simulation
From Atomic to Mesoscale
Can we develop approach to extract relevant macroscopic parameters from simulations based on their significance (e.g. via Fischer information)
Can we refine and improve these predictions by factoring in experimental data (via Bayesian inference)
Theory driven and experiment and history informed materials design
Information compression
Theoretical microscope
Bayesian inference
Coarse graining
Coarse graining
Nanoscale

## Slide 21
Physics-constrained un-mixing
Needs
Bottom electrode
CFO
BFO
A
R1
R2
R2
R1
4D dataset
I = f(x, y, V, Vp)
0
1
2
-5
0
5
time (s)
Voltage (V)
0
1
Current (nA)
Vp
Current-voltage
curves
at each location
x
y
Fitting to physical models
Extracting
Physical meaning
Eigenvector 1
Loading 1
Eigenvector 2
Loading 2
Un-mixing with user-defined constraints on the endmembers or loading maps
Combined spatial and spectral unmixing
Incorporate physics (symmetry, non-negativity, material parameter/models, etc.)
Strelcov et al,
ACS Nano 2014, 2015
Vasudevan et al
submitted
Real space
Spectral space

## Slide 22: Approach
Unsupervised learning, clustering, and visualization
Biggest hurdle: Language/ elementary tools
1. Big data: How does it happen?
Physics informed data analytics/ supervised methods
Biggest hurdles: Mathematical framework, scalability of computational tools
2. Deep data: How can we understand?
Feedback and expert/AI systems
Biggest hurdles: Don’t know where to start, but it is possible
3. Smart data: How can we do better?
Physics: Why something happens
0. Getting big data: making imaging tools a part of data infrastructure

## Slide 23
Level 0: Getting big data
Chemistry
Materials
Science
Global
Security
Biology
Environment
Biomedical
Technology
INSTITUTE FOR FUNCTIONAL
IMAGING OF MATERIALS
Atom Probe
Tomography
Scanning
Probe
Microscopy
Chemical
Imaging
Neutron
Imaging
Data Analytics
Data Modeling
Optical
Imaging
Electron
Microscopy
Mass Spectrometry

## Slide 24
Instrumental limit: photodetector bandwidth (~10 MHz) x DAQ performance (32 Bit)
Single frequency/heterodyne: lock-in compression to ~ 1 kHz
Band excitation: 102 bins at ~ 1 kHz = 100 kHz
Kalinin, Jesse, Proksch, Information Acquisition & Processing in Scanning Probe Microscopy, RD Mag 2008
Data Generation and Utilization in SPM
Single frequency methods:
Band excitation:
We realized we are doing big data
We are losing 99% of data!
Probing local phase transitions requires high (3,4,5,6) D data sets

## Slide 25
Concept and implementation by Stephen “Leonardo” Jesse

## Slide 26
G-mode SPM
Full information capture, lossless compression, and storage of the data stream from the photodetector allowing for:
Recovery of classical SPM
Information theory based analytics and estimating information loss/completeness of classical methods
Physics based analytics
For many SPM modalities, ~1,000 increase of imaging speed
Enables totally new imaging modes
But: need for data analytics and direct streaming to HPC
A. Belianinov et al., Nat. Comm 6, 6550 (2015)
Platform # PCs | Desktop All 5% |  | Supercomputer All 5% | 
Data size | 4 GB |  | 27 GB | 
Duration | ~ 48 hrs | ~ 1 min | 19 min | 8 min
Memory | 40 GB | 6 GB | 173 GB | 115 GB

## Slide 27
Concept and implementation by Stephen “Leonardo” Jesse

## Slide 28
Big Data in Scanning Transmission Electron Microscopy
electron beam
Specimen
STEM for fast data generation:
quantification of beam interaction (pulses),
In-situ movies,
focal series
2D and 3D ptychography
192X192 pixel locations
384X384 pixel scatter-grams
1922X3842= 5X109 data points/scan
2D Ptychography
Sub-Å probe
Advanced
DAQ
Fast Direct
Electron
Detection
To scan coils
CADES

## Slide 29
Instrumental limit: Electron flux (2 108 e/s) x detector performance (1 Bit/electron)
Detectors: Information per electron?
Storage, visualization, and curating
ORNL Solution: BEAM infrastructure
Data Generation in Electron Microscopy
NSRC Workshop on Big, Deep, and Smart Data in Imaging: June 2015, ORNL

## Slide 30
Researcher
Instrument
Control/data acquisition
Community
Social networking/education
Publications/citations
Only small fraction of data stream from the instrumentation is captured
Only small fraction of captured data is analyzed, interpreted, and put in the context
Human-machine interaction during acquisition is often slow and can be non-optimal
Human interpretation of data is limited: bias and ignoring serendipity
Information propagation and concept evolution in scientific community is extremely slow and affected by non-scientific factors
Classical Instrumental Research Paradigm
ms
min
Weeks - months
SPM: 30,000+ platforms worldwide:
Large weakly connected instrumental network
(S)TEM: ~100s top level machines,
much stronger integrated community

## Slide 31
CNMS Researcher
Instrument
Control/data acquisition
User Researcher
Community
Research Paradigm at Facilities such as CNMS

## Slide 32
(geographically) Single large data generation node
Full capture of instrumental data stream
Cloud-based processing and dimensionality reduction
Community-wide analytics
Research Paradigm at Large Facilities

## Slide 33
Multiple geographically-distributed data generation node
Full capture of instrumental data stream /compression/curation
Coordination of protocols and data/metadata across the cloud
Cloud-based processing and dimensionality reduction
Community-wide analytics
Imaging in the Cloud

## Slide 36
Advanced DAQ
To scan coils
electron beam
Bismuth Ferrite Domain Boundary
Ptychography: the D scanning-scattering data set
Sub-Å imaging + Direct Electron Detection + Big data analysis enables effective STEM-ptychography.
Next step: recover physical Information including strain, internal fields, orientation etc.

## Slide 37
STEM/EELS
Transfer files to HPC storage and convert data to HDF5 format
Massively parallel Image processing/ feature detection
Massively parallel electronic structure calculation
High throughput image capture
Multi-modal:
-High-angle annular dark field (HAADF) detector
- Electron energy loss spectroscopy
- O(1000) of images per experiment
Data motion via BBCP/GridFTP
Data conversion from DM3 stacks to HDF5 slices
Standard data format (HDF5)
Data layout conducive to HPC algorithms
Denoise Image
Identify atoms
Identify lattice
Thousands of images/sec
Built on MPI+Fortran
Near linear scaling – some limitations as file counts get extremely large
Massively parallel study of hundreds to thousands of individual configurations
Calculation of electronic structure
Based on Density Functional Theory
0(1000) of configurations
Minutes
Seconds
Minutes
Seconds
Supporting real-time image analytics

## Slide 38
Level 3: Smart Data - Supervised Learning
- Context
- History

## Slide 39
Expert
Control
Automatic
Expert System
Decision making
User
Model
Experimental data
Timeline
X
E
T
R
P
E
From Human Expert to Automatic Systems
Future:
Automated analysis of routine data
Identification of anomalies
Initial training of new practitioners
Data centers: information based on knowledge
Synthesis of expertise: factor in human expert knowledge
Context search: published results data mining/social networks

## Slide 40
Understanding
Data
seed
scale
act
adapt
J. Electron. Imaging. 2012;21(3):033010-1-033010-13. doi:10.1117/1.JEI.21.3.033010
Statistical measures of orientation of texture
for the detection of architectural distortion
in prior mammograms of interval-cancer
Smart data: Google car, cancer screening, expert systems
Notes: (a) Node map for the mammogram shown in Fig. 2. The asterisks (*) represent the peak positions automatically detected in the node map. The numbers next to the asterisks indicate the peaks in descending order of magnitude. (b) The 30 ROIs, each of size 128×128 pixels (except at the edges), obtained by using the peaks detected in the node map. (c) ROIs after FP reduction by using selected features from the set H1, the ANN classifier, and the leave-one-image-out method. Only the top six ROIs are shown in the image at the associated sensitivity of 80% obtained with 5.5 FP/image. The numbers outside the parentheses correspond to the ranking based on the discriminant values obtained by the ANN classifier, and the numbers within the parentheses represent the earlier ranking obtained by phase portrait analysis.
Examples about machine learning
Tourassi
Cancer diagnostics
Google Car
Cat identification

## Slide 41
Timeline
Indirect link
Subject
Material link
Method link
Theory link
Behavior link
Expert evaluation of direct and indirect past knowledge
What makes us a community: structure, correlations, and success in scientific world
S.V. Kalinin and A. Maksov
arXiv:1502.03439

## Slide 42
Citation and semantic analysis of publications
Rapid screening of community for major groups/directions
Evaluation of potential communities of interest (reviewers, latent users)
CiteScape: MRS Fall Tutorial

## Slide 43
From Imaging to Making Stuff
Continuous process monitoring: capture all degrees of freedom we can
Develop materials and synthesis specific schema
Implement across facilities/open format
Data mine prior work/crowd-source for information
Correlative analysis in specific areas/link to structural and thermodynamic data bases
Develop hierarchical clustering approach for materials/methods to integrate communities
Oxides
Nitrides
Sulphides
Films
Crystals
Ceramics
PLD
ALD
MOCVD